## Slide 1
Northern Arizona University
Presentors:
Michael Schubert
Matthew Vigil

## Slide 2
Goals:
Renovate hull design
Brand new mix design
Sustainable building set-up
Project Manager
Matthew Vigil
Project Engineer
Katrina Shurley
Materials Engineer
Michael Schubert
Reinforcement Engineer
Cristopher Aguilar
Structural Engineer
Stephanie Croker

## Slide 3
Hull Dimensions | 
Length | 252 in
Width | 28 in
Height | 16 in
V-Shape
Shallow Concave Bottom
Curved Keel Sailboat
Flat Bottom

## Slide 4
Scenario | Tensile Stress (psi) | Compressive Stress (psi)
Closest To Bow and Stern | 32.2 | 83.6
2-Person | 34.4 | 13.3
4-Person | 102.5 | 39.5
Chart: Length (in)
 | 0.14
Chart: Length (in)
 | -5247.435

## Slide 5
Finishing Mix | 
Wet Unit Weight | 77.8 lb/ft3
Oven-Dry Unit Weight | 64.8 lb/ft3
28-Day Compressive Strength | 3547.0 psi
28-Day Tensile Strength | 321.9 psi
Concrete Air Content | 19%
Structural Mix | 
Wet Unit Weight | 60.3 lb/ft3
Oven-Dry Unit Weight | 53.9 lb/ft3
28-Day Compressive Strength | 1939.0 psi
28-Day Tensile Strength | 218.1 psi
28-Day Flexural Strength | 827.4 psi
Concrete Air Content | 11%

## Slide 8
Wires | Projected (lb) | Expected after losses (lb)
Top | 100 | 80
Middle | 100 | 70
Bottom | 100 | 70