## Slide 1: City of Flagstaff Low Impact Development (LID) Bio-Remediation Soil Design
Final Presentation
Thursday, November 29th, 2018.
Engineering Team:
Meshal Alomar, Abdulrahman Alsubiei, Daniel’le DeVoss, Rebeca Robles
Client and Grading Instructor:
Mark Lamer
Technical Advisor:
Adam Bringhurst

## Slide 2: Low Impact Development (LID) Introduction
CONVENTIONAL SYSTEM
LID
SYSTEM
Pollution Remediation
Pollution Accumulated
Large Volume
Pollution Accumulated
Reduced Volume
Groundwater Recharge
Stormwater Runoff

## Slide 3: Low Impact Development (LID) Introduction
VEGETATION
Figure 1. LID Cross-section
Capstone Project Goals:
  Design a soil matrix with only locally sourced materials
  Design a soil matrix that infiltrates the first inch of stormwater in one hour
  Assess the bio-remediating efficacy
  Assess impact of adding vegetation

## Slide 4: Soil Identification
Soil materials chosen based on the 2017 LID Capstone Final Design Report columns 2 and 6.
Mulch layer avoided since team was growing grass on topsoil for further testing.
Soil materials obtained from The Landscape Connection.
Figure 2. 2017 LID Capstone Final Round Column Designs [1]

## Slide 5: Soil Identification
Material Description | Material Origin
½” to ¼” River Rock | Salt River in Phoenix, AZ
Screened Cinders with 25% to 30% dirt Gravel: Material retained on #4 sieve Sand: Material passing #4 sieve but retained on #40 sieve. | The Landscape Connection Pit in Flagstaff, AZ
Concrete Sand | Dyna Pit in Winslow, AZ
Topsoil Mix with 80% native topsoil and 20% composted mule manure | The Landscape Connection Pit in Flagstaff, AZ
Table 1. Soil Materials Summary [2]

## Slide 6: Grass Layer Assessment
Team wanted to assess the impact of a grass layer on infiltration rates and treatment.
Team selected a native grass mix from Warner’s Nursery in Flagstaff, Arizona.
Origin | Seed Common Name | Mix %
WA | Indian Ricegrass | 19.93
CAN | Sideoats Grama | 19.6
CAN | Fescue Sheep | 11.72
WA | Western Wheat Grass | 11.32
CAN | Blue Grama | 10.75
MN | Bluestern Little | 9.43
NM | Alkali Sacaton | 4.99
TX | James' Galleta | 3.43
CO | Muttongrass | 1.93
- | Inert Matter | 6.85
- | Weed Seed | 0.05
TOTAL |  | 100
Table 2. Native Grass Mix % and Origins [3]
Figure 3. Grown Grass Layer by Rebeca Robles
Notes: BECA

## Slide 7: Soil Testing
Team tested the following on soil materials:
Hydraulic Conductivity
Specific Gravity
Saturated Surface Dry (SSD) Test
Concrete Sand
River Rock
Cinder Sand
Cinder Gravel
Topsoil
Figure 4. Soil Materials by Rebeca Robles
Notes: Test at NAU and WTI

## Slide 8: Hydraulic Conductivity, Void Ratio, and Porosity
Followed ASTM D5856-15
Conducted on all four-soil material (3 tests per type of soil)
* 100%
Void Ratio
Porosity
Hydraulic Conductivity
Density of Soil Sample
Hydraulic Gradient
Figure 5. Hydraulic Conductivity Example [4]
L= Length
V= Volume
A= Area
M1= mass of the permeameter device without soil
M2= mass of the permeameter device with soil
Gs= Specific Gravity
H= Height
Pd= Density of The Compacted Soil
Q= Flow rate
Notes: Explain what M1 and M2 is, the specific gravity from tests performed, explain the difference between h and L using picture.

## Slide 9: Hydraulic Conductivity, Void Ratio, and Porosity Results
Table 3. Hydraulic Conductivity Summary Table
Soil Material | Test # | k (ft/s) | e | n (%)
Screened Cinders | 1 | 0.00149 | 0.25 | 20.009
 | 2 | 0.0012 | 0.148 | 12.873
 | 3 | 0.00127 | 0.218 | 17.902
AVERAGE |  | 0.00132 +/- 0.00015 | 0.205 +/- 0.052 | 16.928 +/- 3.67
1/2" to 1/4" River Rocks | 1 | 0.00151 | 0.255 | 20.314
 | 2 | 0.00136 | 0.231 | 18.772
 | 3 | 0.00136 | 0.255 | 20.314
AVERAGE |  | 0.00141 +/- 0.000087 | 0.247 +/- 0.014 | 19.8 +/- 0.89
Concrete Sand | 1 | 0.00102 | 0.183 | 15.448
 | 2 | 0.00108 | 0.204 | 16.919
 | 3 | 0.00105 | 0.182 | 15.383
AVERAGE |  | 0.00105 +/- 0.000030 | 0.189 +/- 0.012 | 15.916 +/- 0.87
Topsoil Mix | 1 | 0.00014 | 0.284 | 22.107
 | 2 | 0.00014 | 0.255 | 20.306
 | 3 | 0.00014 | 0.318 | 24.127
AVERAGE |  | 0.00014 +/- 0.00 | 0.286 +/- 0.032 | 22.18 +/- 1.91

## Slide 10: Specific Gravity and SSD Test
Followed ASTM C127-15 for coarse aggregates and ASTM C128-15 for fine aggregates.
Conducted only on screened cinders, river rocks, and concrete sand at the Western Technologies Inc. lab and were recommended to not do testing on topsoil.
SSD
Absorption * 100%
Specific Gravity
Saturated Surface Dry Specific Gravity
Absorption
Wd= Mass of dry soil
Wsat= Mass of saturated soil
WSSD = Mass of Saturated surface dry

## Slide 11: Specific Gravity and SSD Test
Material | Test # | Specific Gravity | Specific Gravity (SSD) | Absorption (%)
Screened Cinders | 1 | 2.031 | 2.300 | 8.808
 | 2 | 2.030 | 2.140 | 8.970
 | 3 | 2.032 | 2.190 | 8.990
AVERAGE |  | 2.031 +/- 0.001 | 2.21 +/- 0.082 | 8.923 +/- 0.099
1/2" to 1/4" River Rocks | 1 | 2.567 | 2.799 | 1.469
 | 2 | 2.667 | 2.676 | 1.325
 | 3 | 2.778 | 2.697 | 1.256
AVERAGE |  | 2.671 +/- 0.11 | 2.724 +/- 0.066 | 1.35 +/- 0.11
Concrete Sand | 1 | 2.487 | 2.643 | 2.045
 | 2 | 2.607 | 2.544 | 2.108
 | 3 | 2.578 | 2.654 | 2.044
AVERAGE |  | 2.557 +/- 0.063 | 2.614 +/- 0.061 | 2.066 +/- 0.037
Table 4. Specific Gravity and SSD Summary Table

## Slide 12: Soil Matrix Design
Figure 7. Infiltrated Water Collection by Daniel’le De Voss
2017 LID Capstone Soil Matrix Testing Method [1]:
    Similar to Percolation Test.
  Dry Test
  Saturated Test right after dry test to mimic worst case scenario of multiple storms within a short period of time.
  Void Space Volume Test
Figure 6. Testing Unit by Rebeca Robles
Notes: 6 inch diameter holes, 12 inch deep, performing dry test, and saturated test. Not letting water pond at 12 inches for 24 hourr.

## Slide 13: Soil Media Testing Round #1
Figure 8. Soil Media Testing Round #1 Graph
Designs based on column designs 2017 LID Capstone Final Design Report.
Designs conducted with different sands.

## Slide 14: Soil Media Testing Round #2
Figure 9. Soil Media Testing Round #2 Graph
Experimented with different topsoil mix layer heights and with a topsoil mix with grass layer.

## Slide 15: Soil Media Testing Round #1 and #2 Results
Round #1 |  | 
 | Infiltration Rate (in/hr) | 
Type of Test | Unit 1 (screened cinders sand) | Unit 2 (concrete sand)
Dry Test | 8.95 | 8.55
Saturated Test | 7.96 | 12.54
Table 5. Soil Media Testing Round #1 Results
Round #2 |  |  | 
 | Infiltration Rate (in/hr) |  | 
Type of Test | Unit 3 (2in topsoil) | Unit 4 (1 in topsoil) | Unit 5 (topsoil mix with grass)
Dry Test | 2.98 | 8.30 | 8.82
Saturated | 11.42 | 5.32 | 6.46
Table 6. Soil Media Testing Round #2 Results

## Slide 16: Soil Media Testing Round #3
Round #3 |  |  | 
Test Type | Design #4 Retest #1 | Design #4 Retest #2 | Design #4 Retest #3
Dry Test (in/hr) | 9.49 | 9.44 | 10.01
Saturated Test #1 (in/hr) | 8.98 | 8.99 | 8.12
Saturated Test #2 (in/hr) | 6.45 | 7.04 | 6.87
Void Space Volume (mL) | 1646 | 1543 | 1536
Void Space Volume (mL/ft^3) | 6330.77 | 5934.62 | 5907.69
Round #3 |  |  | 
Test Type | Design #4 with Grass #1 | Design #4 with Grass #2 | Design #4 with Grass #3
Dry Test (in/hr) | 11.24 | 11.49 | 11.04
Saturated Test #1 (in/hr) | 10.92 | 9.13 | 10.3
Saturated Test #2 (in/hr) | 9.86 | 8.66 | 8.78
Void Space Volume (mL) | 1858 | 1755 | 1844
Void Space Volume (mL/ft^3) | 7146.15 | 6750.00 | 7092.31
Retested Design #4, and tested Design #4 with a grass layer
Table 7. Soil Media Testing Round #3 Results
Table 8. Soil Media Testing Round #3 Results (2)
Notes: BECA

## Slide 17: Stormwater Sampling
Figure 10. Contaminating Water by Pouring Over Outdoor Stairs by Daniel’le DeVoss
Figure 11. Contaminating by Pouring Over a Dumpster Lid by Daniel’le DeVoss
Notes: Daniel’le

## Slide 18: Stormwater Testing
Design #4
Design #4
Design #4 with Grass
Design #4 with Grass
1
2
3
1
2
3
1
2
3
1
2
3
Tested the stormwater turbidity, total phosphorus, and total coliform before and after infiltrating it through the soil media columns to assess the columns ability to remediate.
Notes: ADD ASTM Methods

## Slide 19: Turbidity and Total Phosphorous Testing
Figure 12. Untreated and Treated Water Samples by Daniel’le DeVoss
Followed ASTM D6855-12 for Turbidity
Followed HACH Method #10127 for Total Phosphorous
Untreated Water
Water Treated without Grass
Water Treated with Grass

## Slide 20: Coliform Testing
Followed HACH Method #8074
Figure 13. Vacuum Filtration Apparatus By Daniel’le DeVoss
Figure 14. Petri Dishes After Incubation by Daniel’le DeVoss
Untreated Water
Water Treated with Grass
Water Treated without Grass

## Slide 21: Coliform Testing
Figure 15. Diluted Samples and Close-up of Isolated Colonies by Daniel’le DeVoss

## Slide 22: Summary of Water Quality Results
 | Turbidity |  | Total Phosphorus |  | Total Coliform | 
 | NTU |  | mg P/L |  | CFUs/ 100 mL | 
Untreated Water |  |  |  |  |  | 
Average | 864 +/- 45.08 |  | 34.7 +/- 2.71 |  | 404.17 +/- 79.78 | 
After Treatment |  |  |  |  |  | 
 | Grass | No Grass | Grass | No Grass | Grass | No Grass
Average | 86.5 +/- 1.03 | 267.25 +/- 17.97 | 1.47 +/- 0.67 | 3.32 +/- 0.32 | 147.50 +/- 60.53 | 220.83 +/- 40.21
Percent Removal | 90% | 69% | 96% | 90% | 64% | 45%
Table 9. Stormwater Quality Results Summary

## Slide 23: Selecting Final Matrix Design
Design #4 with a Grass Layer was selected as the final soil matrix design:
  Infiltration Rate = 9.1 in/hr
  Storage Capacity = 7.3 L/ft2
  Ability to treat different stormwater contaminants.
  For a proposed Area of 500 ft2:
    Total Water Storage Capacity = 128.47 ft3 or 3,637.86 L
Figure 16. Final Soil Matrix Design

## Slide 24: Project Impacts
Economic Impact
  Prevent infrastructure damages caused by floods.
  Reduce the cost of water treatment
Environmental Impact
  Reduction of sediments, nutrients, and coliform from the stormwater runoff.
Social Impact
  Enhancing community aesthetics using natural elements.
Figure 17. City of Kirkland, WA LID [5]
Figure 18. Concrete stow water
management system [6]
Notes: Meshal

## Slide 25: Project Schedule
Figure 19. Schedule Gantt Chart

## Slide 26: Engineering Work
Estimated Staffing Hours |  |  |  | 
Task | Senior Engineer (hr) | Lab Manager/P.E (hr) | Lab Tech (hr) | Field Tech (hr)
1. Soil Identification | 2 | 2 | 0 | 0
2. Soil Testing | 3 | 3 | 20 | 0
3. Soil Matrix Design | 5 | 10 | 10 | 0
4. Vegetative Coverage Testing | 3 | 10 | 30 | 0
5. Soil Matrix Design Selection | 2 | 5 | 48 | 0
6. Stormwater Run-off Sampling | 2 | 10 | 0 | 40
7. Stormwater Testing | 5 | 7 | 5 | 0
8. Design Economics | 3 | 10 | 0 | 0
9. Selection of Final Soil Matrix Design | 5 | 10 | 5 | 0
10. Project Impacts | 3 | 6 | 0 | 0
11. Project Management | 98 | 98 | 98 | 98
12. Project Deliverables | 36 | 36 | 36 | 36
SUBTOTAL HOURS | 167 | 207 | 252 | 174
 |  |  | TOTAL HOURS | 800
Table 10. Estimated Staffing Hours Table
Notes: Rebeca

## Slide 27: Engineering Work
Actual Staffing Hours |  |  |  | 
Task | Senior Engineer (hr) | Lab Manager/P.E (hr) | Lab Tech (hr) | Field Tech (hr)
1. Soil Identification | 3 | 3 | 0 | 0
2. Soil Testing | 9 | 9 | 9 | 0
3. Soil Matrix Design | 28.5 | 33.5 | 28.5 | 0
4. Vegetative Coverage Testing | 14 | 14 | 45 | 0
5. Soil Matrix Design Selection | 5 | 5 | 25 | 0
6. Stormwater Runoff Sampling | 0 | 0 | 0 | 4
7. Stormwater Testing | 13.5 | 13.5 | 13.5 | 13.5
8. Design Economics | 5 | 5 | 0 | 0
9. Selection of Final Soil Matrix Design | 10 | 10 | 0 | 0
10. Project Impacts | 3 | 3 |  | 0
11. Project Management | 12.5 | 12.5 | 12.5 | 12.5
12. Project Deliverables | 31 | 31 | 31 | 31
SUBTOTAL HOURS | 134.5 | 139.5 | 164.5 | 61
 |  |  | TOTAL HOURS | 499.5
Table 11. Actual Staffing Hours Table

## Slide 28: Engineering Costs
Item | Senior Engineer | Lab Manager/P.E. | Lab Tech | Field Tech
Pay ($/hr) | $92 | $38 | $18 | $18
Multiplier | 1.9 | 2.5 | 3.7 | 3.7
Cost ($/hr) | $175 | $95 | $65 | $65
TOTAL HOURS | 134.5 | 139.5 | 164.5 | 61
SUBTOTAL STAFF COST | $23,511 | $13,253 | $10,651 | $3,950
 |  |  | TOTAL STAFF COST | $51,364
Table 12. Total Staffing Costs Summary Table [7]
Notes: BECA

## Slide 29: Construction Costs
Excavation Cost | 
Price Per Hour | 9 $/cu. yd
Total Excavation Hours | 19 cu. yd
Total Excavation Cost | $171.00
Table 13. Total Excavation Cost Summary Table [8]
Grass Costs | 
Grass Coverage | 1000 ft^2/lb
Cost Per Pound | 39.99 $/lb
Grass Coverage Area | 500 ft^2
Grass Needed | 0.5 lbs
Total Grass Cost | $20.00
Table 14. Total Grass Cost Summary Table [4]
Soil Materials Cost |  |  |  |  | 
Layer | Area (ft^2) | Volume (ft^3) | Volume (cu. yd.) | Cost ($/cu. yd.) | Cost ($)
Topsoil Mix with Grass | 500 | 41.67 | 1.54 | $14.00 | $21.60
Screened Cinder Sand | 500 | 312.50 | 11.57 | $9.75 | $112.85
Screened Cinder Gravel | 500 | 83.33 | 3.09 | $10.50 | $32.41
1/2" to 1/4" River Rock | 500 | 83.33 | 3.09 | $38.95 | $120.22
 |  |  |  | Total Soils Cost | $287.08
Table 15. Total Soil Materials Cost Summary Table [2]

## Slide 30: References
[1] R. Pott; T. Alhamidi; F.DiFore; Z.Zhang. “CENE 486 Final Capstone Report: Low Impact Development Bio-Remediation Soil Design.” 2017.
[2]Connection, T. (2010). Materials List. [online] The Landscape Connection. Available at: https://www.landscapeconnection.biz/materials-list.html [Accessed 10 Nov. 2018].
[3] Warner’s Nursery. (2018). Grass Compositions and Prices.
[4] https://knowledge4civil.wordpress.com/2016/12/11/flow-of-water-through-soil/
[5] “Low Impact Development,” City of Kirkland official website. [Online]. Available: https://www.kirklandwa.gov/depart/Public_Works/Utilities/Storm___Surface_Water/Development_and_Construction/Low_Impact_Development.htm.
[6] “What Does the Storm Drainage System Look Like?,” Fairfax County Virginia. [Online]. Available: https://www.fairfaxcounty.gov/publicworks/stormwater/what-does-storm-drainage-system-look.
[7] “ PROFESSIONAL CONSTRUCTION MATERIALS ENGINEERING & TESTING SERVICE FEE SCHEDULE FOR NOBLE MIDSTREAM SERVICES, LLC,” p. 2016, 2016.
[8] 108 excavating. (2017). 108 EXCAVATING. [online] Available at: http://www.108excavating.com/ [Accessed 28 Nov. 2017].