## Slide 1
By: Roy Crouch, Stephen Gergal, Fernando Rojo, and Brandy Wagoner
UGRADS, PCI Big Beam Competition
4-26-2018

## Slide 2: Project Background
PCI is a technical institute for the Precast/Prestressed Concrete industry.
This is the 9th year that NAU will be competing.
This project is generously sponsored by Tpac, an Encon company.
Figure 1: Precast/Prestressed Concrete Institute logo [1]
Figure 2: Northern Arizona University CEFNS logo [2]
Figure 3: TPAC logo [3]

## Slide 3: Precast/Prestressed Concrete
Precast - Concrete elements are cast off-site and shipped to the final in-service location.
Prestressed - Structural elements consist of reinforcing steel and high-strength steel strands which are pretensioned before the concrete is cast, and cut once the concrete has reached a certain strength. They apply a compressive force on the member, allowing it to carry greater loads and span greater distances than mildly reinforced members.
Figure 4: Prestressing strand anchoring device (photo by Roy Crouch)
Notes: I think this slide has to many words, should we try to shorten it out?

## Slide 4: The Competition
Competition Design Objective
Design a precast/prestressed beam for a cracking capacity of 20 kips and an ultimate capacity between 32 and 39 kips, while minimizing cost and weight and maximizing deflection for prescribed loads.
Judging Criteria
Design accuracy.
Lowest cost.
Lowest weight.
Largest measured deflection at maximum total applied load.
Most accurate prediction.
Report quality.
Practicality, innovation, and conformance to code.
Figure 5: Tpac logo [1]
Figure 6: Northern Arizona University logo [2]

## Slide 5: Mix Design
Figure 7: Broken Cylinder after compressive test (taken by Stephen Gergal)
*Pumice used as aggregate
Table 1: Concrete mixes
Normal Weight Mixtures | Cement | Fly Ash | Normal Weight Coarse Aggregate | Fine Aggregate | W/C Ratio
Tpac NW | 730 | 185 | 1,484 | 1,268 | 0.31
NAU #1 NW | 623 | 267 | 1,550 | 1,288 | 0.30
NAU #3 NW | 600 | 356 | 1,390 | 1,360 | 0.29
LightweightMixtures | Cement | Fly Ash | Lightweight Coarse Aggregate | Fine Aggregate | W/C Ratio
Tpac LW | 730 | 185 | 867 | 1,328 | 0.34
NAU #2 LW | 610 | 261 | 150* | 1,200 | 0.31
NAU #4 LW | 600 | 356 | 940 | 1,070 | 0.34
Notes: Can we add a table here to show everyone what each mix was made of? Like cement type, aggregate, and pozzolan?

## Slide 6: Mix Testing Results
Table 2: Mix testing results
Normal Weight Mixtures | Unit Weight (pcf) | Compressive Strength (psi) | Tensile Strength (psi) | Modulus of Elasticity (ksi)
Tpac NW | 148.3 | 10,000 | 349 | 5,700
NAU #1 | 148.1 | 7,130 | 474 | 4,813
NAU #3 | 147.3 | 2,360 | 239 | 2,769
Lightweight Mixtures | Unit Weight (pcf) | Compressive Strength (psi) | Tensile Strength (psi) | Modulus of Elasticity (ksi)
Tpac LW | 126.0 | 8,000 | 505 | 5,098
NAU #2 | 126.8 | 1,312 | 230 | 2,064
NAU #4 | 118.1 | 1,526 | 150 | 2,227
Compressive strength test
Tensile strength test
Photo courtesy: Fernando Rojo
Photo courtesy: Fernando Rojo
Notes: This slide would need just a table, showing the results from each test done

## Slide 7: Mix Scoring
Table 3: Concrete Mix Decision Matrix
*LW - Lightweight concrete mix
*NW – Normal weight concrete mix
Mixes | Unit Weight (pcf) | Rank | Compressive Strength (psi) | Rank | Tensile Strength (psi) | Rank | Modulus of Elasticity (ksi) | Rank | Score
Tpac NW | 148.3 | 1 | 10,000 | 6 | 349 | 4 | 5,700 | 1 | 3.5
NAU #1 NW | 148.1 | 2 | 7,130 | 4 | 474 | 5 | 4,813 | 3 | 3.75
NAU #3 NW | 147.3 | 3 | 2,360 | 3 | 239 | 3 | 2,769 | 4 | 3.3
Tpac LW | 126 | 5 | 8,000 | 5 | 505 | 6 | 5,098 | 2 | 4.35
NAU #2 LW | 126.8 | 4 | 1,312 | 1 | 230 | 2 | 2,064 | 6 | 3.05
NAU #4 LW | 118.1 | 6 | 1,526 | 2 | 150 | 1 | 2,227 | 5 | 3.05
Weighted Factor |  | .10 |  | .35 |  | .25 |  | .30 | 
Notes: Decision matrix of how we chose the TPAC LW mix

## Slide 8: Final Mix Design: TPAC’s LW Mix
Table 4: Tpac LW Composition
Material | Weight (lbs/CY) | Volume (CF/CY)
Cement | 730 | 3.71
Admixture (30% Fly Ash) | 185 | 1.35
Coarse Aggregate | 867 | 8.58
Sand | 1,328 | 8.15
Water | 308 | 4.94
Air Entrainment | 1% | 0.27
Admixtures | 
Advacast 575 | Improves Workability
VmarF 100 | Improves Consolidation
Recover | Stabilizes Hydration
3 Day Strength (psi) | 5,000
28 Day Strength (psi) | 8,000
W/C Ratio | 0.337
Unit Weight (pcf) | 126.0
Table 5: Tpac LW Characteristics
Notes: Give details about mix design, very large writing, and easy to read table.

## Slide 9: Cross Section Design
MathCAD model is designed to analyze:
  Stresses at release
  Cracking load
  Ultimate capacity
  Shear capacity
Each cross section is analyzed for:
  20 kip cracking capacity
  Ultimate failure between 32 and 39 kips
Scoring = (value- worst value)
(best value - worst value)
Decision matrix is scored on:
  Lowest cost
  Lowest weight
  Largest deflection

## Slide 10: Beam Scoring
Table 6: Decision matrix for the selection of a cross section using parameters defined by PCI.
X-Section Considered | Cost ($) | Rank | Weighted Factor | Weight of Section (plf) | Rank | Weighted Factor | Defl. (in) | Rank | Weighted Factor | Total Score
I Beam #1 | 71 | 5 | 0.745 | 108.0 | 6 | 0.306 | 0.019 | 3 | 0.579 | 1.629
I Beam #2 | 62 | 4 | 0.929 | 78.00 | 4 | 0.833 | 0.010 | 8 | 0.078 | 1.839
I Beam #3 | 59 | 2 | 0.997 | 69.00 | 2 | 0.996 | 0.017 | 6 | 0.495 | 2.489
Box Beam #1 | 100 | 9 | 0.116 | 126.0 | 10 | 0.000 | 0.023 | 2 | 0.795 | 0.911
Bulb T | 60 | 3 | 0.964 | 75.00 | 3 | 0.882 | 0.009 | 9 | 0.016 | 1.862
C Beam | 79 | 6 | 0.560 | 108.0 | 5 | 0.318 | 0.011 | 7 | 0.085 | 0.963
* Box Beam #2 | 59 | 1 | 1.000 | 68.00 | 1 | 1.000 | 0.018 | 5 | 0.520 | 2.520
I Beam #4 | 80 | 7 | 0.549 | 109.00 | 7 | 0.302 | 0.008 | 10 | 0.000 | 0.852
I Beam #5 | 106 | 10 | 0.000 | 125.00 | 9 | 0.006 | 0.027 | 1 | 1.000 | 1.003
T Beam | 89 | 8 | 0.366 | 120.00 | 8 | 0.114 | 0.018 | 4 | 0.522 | 1.002
* Selected cross section

## Slide 11: Final Beam Design
Materials:
  Tpac’s light weight concrete
  #4 Compression Steel
  Prestressing strands
  Welded Wire Fabric (WWF)
  Styrofoam in void
Design:
  Concrete unit weight:126 pcf
  Total weight: 1,500 lbs
  Prestressing strands pulled to 31 kips each
Figure 8: Final cross section design of beam
Void

## Slide 12: Beam Fabrication
Figure 11: Concrete beam being cast in the custom built form. Picture courtesy of Brandy Wagoner
Figure 10: Top view of beam before casting. Picture courtesy of Brandy Wagoner
Figure 9: End view of beam before casting. Picture courtesy of Brandy Wagoner

## Slide 13: Final Beam
Figure 12: Beam casting, still inside form.
Photo Courtesy: TPAC
Figure 13: Beam sitting outside NAU concrete lab
Photo Courtesy: Fernando Rojo

## Slide 14: Prediction Calculations
Equation 1: Failure Load
Equation 2: Cracking Load
Equation 3: Stresses experienced

## Slide 15: Staffing
Table 7: Actual total project hours
Table 8: Predicted total project hours
Staffing |  |  |  |  | 
Task | S. ENG | ENG | Lab | AA | Total
Mix Design | 15 | 50 | 45 | 20 | 130
Mix Testing | 5 | 35 | 95 | 10 | 145
Beam Design | 15 | 45 | 8 | 5 | 73
Beam Manufacturing | 5 | 20 | 10 | 8 | 43
Prediction Calculations | 20 | 40 | 5 | 5 | 70
Testing | 10 | 40 | 90 | 10 | 150
Report | 12 | 35 | 15 | 35 | 97
Total Hours | 82 | 265 | 268 | 93 | 708
Staffing |  |  |  |  | 
Task | S. ENG | ENG | Lab | AA | Total
Mix Design | 15 | 45 | 45 | 20 | 125
Mix Testing | 5 | 30 | 85 | 10 | 130
Beam Design | 15 | 40 | 5 | 5 | 65
Beam Manufacturing | 5 | 15 | 6 | 5 | 31
Prediction Calculations | 18 | 35 | 5 | 5 | 63
Testing | 10 | 35 | 80 | 10 | 135
Report | 10 | 30 | 10 | 25 | 75
Total Hours | 78 | 230 | 236 | 80 | 624
S. Eng = Senior Engineer
ENG = Engineer
LAB = Lab Technician
AA = Administrative Assistant

## Slide 16: Cost
Table 9: Actual cost of project
Budget |  |  |  | 
Staffing | Personal | Hours | Billing Rate ($/hr) | Cost ($)
 | S. ENG | 78 | 130 | 10,140
 | ENG | 230 | 70 | 16,100
 | LAB | 236 | 40 | 9,440
 | AA | 80 | 35 | 2,800
Lab Use |  | 75 | 100 | 7,500
Beam Fabrication/Shipping |  |  |  | 5,000
Travel Costs |  |  |  | 400
Total cost of project ($) |  |  |  | 51,380
Budget |  |  |  | 
Staffing | Personal | Hours | Billing Rate ($/hr) | Cost ($)
 | S. ENG | 82 | 130 | 10,660
 | ENG | 265 | 70 | 18,550
 | LAB | 268 | 40 | 10,720
 | AA | 93 | 35 | 3,255
Lab Use |  | 90 | 100 | 9,000
Beam Fabrication/Shipping |  |  |  | 5,000
Travel Costs |  |  |  | 400
Total cost of project ($) |  |  |  | 57,585
Table 9: Predicted cost of project

## Slide 17: Schedule
Table 9: Project Schedule
Task | Anticipated end date | Actual end date
Mix Test results | 01-19-2018 | 01-19-2018
Mix Selection | 01-26-2018 | 01-26-2018
MathCad Model | 01-26-2018 | 01-26-2018
Beam Selection | 01-31-2018 | 02-20-2018
Shop Drawing | 02-14-2018 | 03-06-2018
Prediction Calculations | 02-14-2018 | 02-14-2018
Beam Manufacturing | 03-8-2018 | 04-06-2018
Testing | 03-19-2018 | 05-04-2018
Video | 03-22-2018 | 05-07-2018
Final Report (NAU) | 04-2-2018 | 05-10-2018
Final Report (PCI) | 04-6-2018 | 05-10-2018

## Slide 18: References
[1] TPAC, "TPAC Official Website," [Online]. Available: tpacaz.com. [Accessed 30 11 2017].
[2] Northern Arizona University, "NAU CEFNS," 21 04 2018.
[3] Precast/Prestressed Concrete Institute, "PCI," [Online]. Available: pci.org.
[Accessed 30 11 2017].
[4] PCI, "2018 PCI Big Beam Brochure," [Online]. [Accessed 30 11 2017].