## Slide 1: CENE 486C Final Presentation Concrete Canoe: Agassiz
By: Stephan Henderson, Logan Grijalva, Kristen Rasmussen, Conrad Senior, Carl Wilson
Date: 4/24/2020
Notes: Hi Everyone! Were are the 2020 Concrete Canoe Team – Agassiz

## Slide 2: Project Introduction
Design, Build, and Race a Concrete Canoe
NCCC publishes a Request for Proposal document that all teams must abide by
Compete at the Pacific Southwest Conference at California State University, Fullerton on April 1- 4
Figure 1: NCCC Request for Proposals [1]
Notes: The goal of this project is to design, build and race a concrete canoe. The canoe was constructed based on requirements given by the National Concrete Canoe Committee. We will compete at the Pacific Southwest Conference at California State University-Fullerton from April 1st-4th

## Slide 3: Task 1: Mix Material Acquisitions
Figure 2: Uncrushed Ultralightweight Foamed Class Aggregate (UL FGA)
Photo Credit: Conrad S.
Figure 3: Crushed UL-FGA
Photo Credit: Conrad S.
Figure 5: Drying Wet Ul-FGA
Photo Credit: Conrad S.
Figure 4: Dry Sieving
Photo Credit: Conrad S.
Notes: To obtain Utelite, Silica Fume, Fly ash, Cement, admixture, color supplier and manfacturers were contacted
Aeroaggrate made to be crushed and sieved to pass Conference requirements
Figure 2 shows the uncrushed aeroaggregate
Figure 3 shows the aggregate after it has gone through a jaw crusher
Figure 4 shows the sieve that was to dry sieve the crushed aggregate
Figure 5 shows the aggregate drying at Western Tech after it was sieved through the on the #200 sieve

## Slide 4: Task 1: Alternative Mix Designs
Table 1: C/CM Ratio & Aggregate Gradation |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | Unit Weight (pcf)
4 | 12% C/CM | 600 | 70
5 | 70% C/CM | 3970 | 73
6 | 55% C/CM | 3020 | 73
7 | 40% C/CM | 910 | 74
Table 1: C/CM Ratio & Aggregate Gradation |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | 
4 | 12% C/CM | 600 | 70
5 | 70% C/CM | 3970 | 73
6 | 55% C/CM | 3020 | 73
7 | 40% C/CM | 910 | 74
Figure 6: Mix 4
Photo Credit: Conrad S.
Figure 7: Mix 5
Photo Credit: Conrad S.
Figure 8: Mix 6
Photo Credit: Conrad S.
Figure 9: Mix 7
Photo Credit: Conrad S.
Notes: Goal of the Mix Design was to make a mix more sustainabe by using by products and recycled materials( silica fume, fly ash and Aeroaggregate)
The C/CM ratio was tested to determine the best relationship between strength and weight
The following ratios were tested based on research

## Slide 5: Task 1: Alternative Mix Designs
Table 1: C/CM Ratio & Aggregate Gradation |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | Unit Weight (pcf)
4 | 12% C/CM | 600 | 70
5 | 70% C/CM | 3970 | 73
6 | 55% C/CM | 3020 | 73
7 | 40% C/CM | 910 | 74
Table 1: C/CM Ratio & Aggregate Gradation |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | 
4 | 12% C/CM | 600 | 70
5 | 70% C/CM | 3970 | 73
6 | 55% C/CM | 3020 | 73
7 | 40% C/CM | 910 | 74
Figure 6: Mix 4
Photo Credit: Conrad S.
Figure 7: Mix 5
Photo Credit: Conrad S.
Figure 8: Mix 6
Photo Credit: Conrad S.
Figure 9: Mix 7
Photo Credit: Conrad S.
Notes: The selected mix was number 6 at a C/cm ratio of 55%
Due to its strength was enough to support the paddlers

## Slide 6: Task 1: Alternative Mix Design Cont.
Table 2: Aggregate Graduation |  |  | 
Mix Number | Characteristic of Interest | 28 day Compressive Strength (psi) | Wet Unit Weight (pcf)
9 | Well Graded Utelite | 2460 | 63
10 | No Crushed Fines | 1720 | 63
11 | Low #10 Mesh | 1700 | 63
Figure 10: Compressive Testing
Photo Credit: Conrad S.
Notes: Strength of Aggregates graduations testing.
Different proportions of each size were used
Sizes (crushed fines,fines, 10 mesh)

## Slide 7: Task 1: Alternative Mix Design Cont.
Table 2: Aggregate Graduation |  |  | 
Mix Number | Characteristic of Interest | 28 day Compressive Strength (psi) | Wet Unit Weight (pcf)
9 | Well Graded Utelite | 2460 | 63
10 | No Crushed Fines | 1720 | 63
11 | Low #10 Mesh | 1700 | 63
Figure 10: Compressive Testing
Photo Credit: Conrad S.
Notes: The selected sizes are utelite would be equal proportions of each was the best

## Slide 8: Task 1: Alternative Mix Design Cont.
Table 3: Weight Reduction Trials |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | Wet Unit Weight (pcf)
12 | 550 lbs of C/CM, Well Graded Utelite, No Crushed Fines | 1700 | 56
13 | 550 lbs of C/CM, Well Graded Utelite Aggregate | 1710 | 56
14 | 600 lbs of C/CM, Well Graded Utelite Aggregate | 2110 | 56
Figure 11: Mix 12
Photo Credit: Conrad S.
Figure 12: Mix 13
Photo Credit: Conrad S.
Notes: The weight of the mix was still to high, to reduce weight more three options were tested listed above.
Reduce CM or aggreate or higher aggregate used done to test strength coming from cement or aggregate was greater

## Slide 9: Task 1: Alternative Mix Design Cont.
Table 3: Weight Reduction Trials |  |  | 
Mix Number | Characteristic of Interest | 28-day Compressive Strength (psi) | Wet Unit Weight (pcf)
12 | 550 lbs of C/CM, Well Graded Utelite, No Crushed Fines | 1700 | 56
13 | 550 lbs of C/CM, Well Graded Utelite Aggregate | 1710 | 56
14 | 600 lbs of C/CM, Well Graded Utelite Aggregate | 2110 | 56
Figure 11: Mix 12
Photo Credit: Conrad S.
Figure 12: Mix 13
Photo Credit: Conrad S.
Notes: The best to keep the strength was mix 14
So 600 lbs for C/CM material would be used with Well graded utelite.

## Slide 10: Task 1: Alternatives Mixes Cont.
Table 4: Additional Water Results |  | 
Mix Number | Amount of Water Reducer (fl. oz/cwt) | Additional Water (grams/cf)
15 | 12 | 1300
16 | 13 | 700
17 | 14 | 290
Figure 13: No Slump
Photo Credit: Conrad S.
Figure 14: Low Slump
Photo Credit: Conrad S.
Figure 15: High Slump
Photo Credit: Conrad S.
Notes: To test workability slump test were conducted
To retain strength, water reducer was added outside of the recommended range to not allow for excess water to be used.
Excess water water lowers the strength of the concrete by over saturatignt he cement particle so the mix does have an evenly distributed cement
Measured in grams per cubic foot

## Slide 11: Task 1: Alternatives Mixes Cont.
Table 4: Additional Water Results |  | 
Mix Number | Amount of Water Reducer (fl. oz/cwt) | Additional Water (grams/cf)
15 | 12 | 1300
16 | 13 | 700
17 | 14 | 290
Figure 13: No Slump
Photo Credit: Conrad S.
Figure 14: Low Slump
Photo Credit: Conrad S.
Figure 15: High Slump
Photo Credit: Conrad S.
Notes: 14 was the dosage used for the water reducer

## Slide 12: Task 1: Alternative Mix Designs Cont.
Table 5: Color Trials |  | 
Mix Number | Percent of Color Added | Cement Color
18 | 2% | White
19 | 2% | Gray
20 | 5% | White
21 | 5% | Gray
22 | 6% | White
Figure 18: Final Concrete Colors
Photo Credit: Conrad S.
Figure 17: 2% Trials
Photo Credit: Conrad S.
Figure 16: 5% Color Trials
Photo Credit: Conrad S.
Notes: To get the best color of the mix varying colors dosages and color of the cement were tested
Dosages were based off of the color recommendations

## Slide 13: Task 1: Alternative Mix Designs Cont.
Table 5: Color Trials |  | 
Mix Number | Percent of Color Added | Cement Color
18 | 2% | White
19 | 2% | Gray
20 | 5% | White
21 | 5% | Gray
22 | 6% | White
Figure 18: Final Concrete Colors
Photo Credit: Conrad S.
Figure 17: 2% Trials
Photo Credit: Conrad S.
Figure 16: 5% Color Trials
Photo Credit: Conrad S.
Notes: Final colors of the concrete can be seen in figure 18

## Slide 14: Task 1: Final Mix Quantities
Table 6: Solid Materials | 
Materials | Quantity (lb/cyd)
White Cement | 340
Class F Fly Ash | 180
Waterproofing Admixture | 6.8
Silica Fume | 90
Poraver (1-2 mm) | 160
Poraver (0.1-0.3 mm) | 70
Poraver (0.25-0.5 mm) | 120
UL-FGA (#8-#200) | 190
Utelite Fines (#4-#20) | 30
Utelite #10 Mesh (#50-#200) | 30
Utelite Crushed Fines | 30
MasterFiber M100 | 0.5
Interstar Blue Color | 37.01
Table 7: Liquid Materials | 
Materials | Quantity (fl. oz/cwt)
MasterSet Delvo (Retarder) | 5
Master Glenium 7500 (Water Reducer) | 14
MasterLife SRA 35 (Shrinkage Reducer) | 5
Figure 19: Floating Concrete
Photo Credit: Conrad S.
Notes: The final quantities to make 1 cubic yard
Table 6 shows the amount of dry materiasl in pound per cubic yard
Table 7 shows the the amount of liquid materials in fluid ozunces per hundred of CM
Concrete floats

## Slide 15: Task 1: Concrete Strength Testing
Table 8: Strength Results |  | 
Concrete Mix | Interior Mix (White) | Exterior Mix (Blue)
Unit weight | 56.1 | 56.2
Compressive Strength ( 7 day) | 1140 psi | 1230 psi
Compressive Strength (28 day) | 2110 psi | 2110 psi
Tensile Strength | 180 psi | 180 psi
Flexural Strength | 2080 psi | 2080 psi
Table 8: Strength Results |  | 
Concrete Mix | Interior Mix (White) | Exterior Mix (Blue)
Unit weight |  | 
Compressive Strength ( 7 day) | 1140 psi | 1230 psi
Compressive Strength (28 day) | 2110 psi | 2110 psi
Tensile Strength | 180 psi | 180 psi
Flexural Strength | 2080 psi | 2080 psi
Figure 20: Flexural Testing
Photo Credit: Conrad S.
Figure 22: Compressive Testing
Photo Credit: Conrad S.
Figure 23: Tensile Test Cylinder
Photo Credit: Conrad S.
Figure 21: Concrete Cylinders
Photo Credit: Conrad S.
Notes: Summary of the strenght of the final mix and the corresponding test setup

## Slide 16: Task 2: Final Hull Design Development
Final Canoe Dimensions |  | 
Length | 212.5 | Inches
Width (Middle) | 27.52 | Inches
Depth | 14.2 | Inches
Thickness | 0.5 | Inches
Weight | 160 | Pounds
Figure 24: SolidWorks Analysis Data Sheet
SolidWorks Development
Table 9: Final Canoe Dimensions
Notes: The second task for this project included Hull Development
The hull for the canoe was designed in SolidWorks due to the ease of adjusting the design.
Figure 24 illustrates the Analysis data sheet that was acquired after each new design. These values were used in conjunction with the structural calculations to determine the varies properties of the canoe.
Figure 24 is present on the slide to demonstrate that an analysis was run for the hull design through SolidWorks
Table 9 demonstrates a simplified table of the values that were derived from Figure 24. These values include the Length, Width ( At Middle), Depth, The Average Thickness, and the Theoretical Weight of the Canoe.

## Slide 17: Task 2: Final Hull Design Development
Figure 25: Isometric Canoe Image
SolidWorks Development
Notes: The competition of the Hull Design is illustrated in Figure 25. This figure demonstrates an Isometric rendition of the Proposed Canoe in SolidWorks.

## Slide 18: Task 2: Final Mold Development
Full Size Mold
64 Cross Section
4 in Thickness
Mold Utilized 1.5 Density Foam
Expanded Polystyrene (EPS) Foam
Manufacture: EPS Products
Will be used to Create Final Canoe
Half Size Mold
32 Cross Section
4 in Thickness
Mold Utilized 1.5 Density Foam
Expanded Polystyrene (EPS) Foam
Manufacture: EPS Products
Will be used for Practice Canoe and to develop Standard Operating Procedures (SOP) for Full Size Canoe
Notes: Once the hull was finalized, the mold development could begin
A half-sized mold and a full-size mold was developed.
The half size was developed with the utilization of 32 cross-sections, which were constructed utilizing 1.5 lb/ft^3 Expanded Polystyrene Foam.
Cross-sections were 4 inches thick, and EPS Products manufactured the Mold.
The half-Sized mold was utilized to develop Standard Operating Procedures (SOP's) to be utilized for the full-size canoe.
The full-size canoe utilized the same material and thickness of each cross-section but had a total of 64 cross-sections.
The full-size mold was utilized in producing the final concrete canoe

## Slide 19: Task 2: Final Mold Development
Figure 26: Isometric Mold Image Full Size
SolidWorks Development
Notes: Figure 26 demonstrates the isometric view of the final mold development for the full-size canoe. This mold was developed in SolidWorks and demonstrates how the cross-sections are developed in the mold.
Note that some cross-sections are smaller due to the geometry of the canoe.
Smaller cross-sections better reflect the geometry of the canoe at that point.

## Slide 20: Task 2: Mold Procurement
Notes: The drawing shown is an example of the cross-sections that were developed for EPS Products. Every cross-section had to be sent separately for both the full size and half size canoe.
The correct scale and cross-section had to be developed by exporting the mold out of SolidWorks and revised in AutoCAD.
The measurements that are shown are only for reference.
To construct these cross section, a scaled printout in conjunction with a hot knife was used for each cross-section.
Due to the limitation of the machine used, a 2D model at 4-inch thickness was developed.
This involves sanding to finish when the mold is developed.

## Slide 21
Notes: This construction drawing demonstrates sheet 1 of 2 for the developed construction drawings.
The top of the drawing demonstrates a plan and profile view of the canoe. This demonstrates the different section cuts used to show certain features of the canoe, and dimensions of the canoe.
Section A-1 in the bottom left corner demonstrates a section cut that involves the installation of the bulkhead.
Section B-1 in the bottom right hand corner demonstrates the cross-section profile of the canoe in between the bulkheads.

## Slide 22
Notes: Sheet 2 of 2 demonstrates certain details to help aid the section cuts, and an isometric view of the canoe and mold that was developed in SolidWorks.
The isometric view demonstrates how the mold, section cuts, and the canoe will interact. The canoe has been lifted from the mold slightly in the model to see the different components and how they interact.
Detail 1 illustrates how the material is layered into the mold, where the bulkhead is installed.
Detail 2 demonstrates the layering in the material, but without the bulkhead.
The Notes and Bill of Materials on the right-hand side of the drawing demonstrates and certain call outs or details that need to be known for the project.

## Slide 23: Task 3: Structural Analysis Calculations
Assumptions
  Symmetrical U-shaped Beam
  200 lb paddler weight acting as point loads at 15% and 85% of the length
  Uniform distributed buoyancy force acting as reaction
Analysis
  Completed in Microsoft Excel
  Dependent on Mix Design strength and Hull Design geometry
  Conformed to RFP requirements set forth by NCCC
    Ex. 5 ft long 80 lb/ft distributed load acting at the middle
Notes: In order to analyze the canoe the best we could, we had to make a few assumptions. The first assumption is a "U" shaped cross section that has 90-degree corners and straight edges, with constant geometric properties along the entire length of the canoe. The other 2 assumptions for analyzing the canoe is a paddler weight of 200 pounds that act as point loads at 15 and 85 percent of the canoe's length and finally the buoyancy force on the bottom of the canoe acting as the reaction force.

## Slide 24: Task 3: Structural Calculations
Design Criteria | Value
Canoe Weight (lb/ft) | 10.7
Depth in Water at Equilibrium (in) | 9.49
Buoyancy Force (lb/ft) | 55.93
Centroid (in) | 3.85
Moment of Inertia (in^4) | 561.13
Design Variable | Capacity | Experienced Load
Moment (lb*ft) | 935.04 | 283.57
Compressive Stress (psi) | 2100 | 62.52
Tensile Stress (psi) | 183.3 | 23.35
Shear Stress (psi) | 68.74 | Keel: 2.97 Gunwale: 1.06
Table 10: Design Criteria Values
Table 11: Design Variable Values
Notes: The values in the design criteria table were used in calculations to obtain design variables. The design criteria values were acquired from the hull and mix design and then calculations were performed to ensure the capacity of the canoe exceeds the experienced load the canoe with undergo. These designs variables were chosen because they are the most detrimental to the structural integrity of the canoe. As you can see, the capacity values well exceed the experienced load, which means based on our calculations the canoe will not fail structurally.

## Slide 25: Profile Free Body Diagram
Figure 27: Profile Free Body Diagram
Notes: The figure here shows the profile view free body diagram. The canoe weight is depicted in the blue distributed load while the green distributed load represents the buoyancy force. The gray loads are required loads from the request for proposal from the NCCC and had to be a part of the analysis. Finally the gray dimensions depict the geometry of the canoe.

## Slide 26: Cross Section Free Body Diagram
Figure 28: Cross Section Free Body Diagram
Notes: The figure above shows the cross section of the canoe. This figure depicts the assumed U section. The green loads represent the water pressure as a distributed load on the walls of the canoe and the black dimensions represent the square geometry. The buoyancy and self weight of the canoe were not shown in this figure because the design values related to those loads were calculated based on the profile view free body diagram.

## Slide 27
Figure 29: Shear Force Diagram
Notes: The figure above is the shear diagram and represents the shear in pounds in respect the length along the canoe in feet. For example, at just shy of 3 feet the shear is roughly 120 pounds and then drops to roughly negative 80 pounds due to the paddle sitting in this location. The relationship is linear because the loading is distributed and shift to vertical at the location of the paddlers.

## Slide 28
Figure 30: Bending Moment Diagram
Notes: The figure above shows the moment diagram in pound-feet units in respect to the length along the canoe in feet. For example, the moment directly in the middle of the canoe is roughly 280 pound-feet and this calculations is reflected in the design variables under the experienced loading column. This relationship is parabolic because the integral of shear is moment, which reflects the distributed load acting on the canoe.

## Slide 29: Task 4: Mold Construction
Figure 31: Shadow Sanding of Final Mold ​
Figure 32: Flex Sealing the Mold After Sanding
Notes: To begin the construction of the canoe the mold was glued together and shadow sanded smooth as seen in Figure 31 and 32. Then the foam mold was covered with a layer of Flex Seal. The Flex Seal was used to prevent water from seeping into the mold and to aid with releasing the canoe from the mold.

## Slide 30: Task 5: Final Canoe Construction
Figure 33: Applying Vaseline to Mold for Release Agent ​
Figure 34: Inserting Mesh Cage After ​First Layer of Concrete
Notes: Figure 33 shows the Vaseline that was applied to the mold to aid in an easy release of the canoe from the mold. Then the first layer of concrete was applied. This concrete was colored blue for aesthetic purposes. After the first layer was complete the basalt mesh was placed into the concrete as seen in Figure 34. Each layer of concrete had to be a ¼’ thick to achieve the ½” canoe thickness. This was measured with wooden paint sticks. The team decided that paint stick were the best tool to measure because there was no worry about pushing the pant sticks into the foam mold and getting incorrect measurements.

## Slide 31: Task 5: Final Canoe Construction Cont.
Figure 35: Applying Mesh Reinforcement to the Bow and Stern ​
Figure 36: Installing Gunwale Mesh for Extra Protection ​
Notes: Figure 35 and 36 shows the team installing the mesh. As seen the team used claps to hold the mesh in place so that the spacing was correct. For reinforcement, the team placed reinforcement at the spine, gunwales, a full cage and around the bulk heads. The gunwales, spine and the ending on the bulkheads showed to be the weakest points of the canoe it is for this reason that the team placed extra reinforcement at these locations.

## Slide 32: Task 5: Final Canoe Construction Cont.
Figure 37: Tamping Concrete into Bulkhead to ensure Good Consolidation ​
Figure 38: Applying Second Layer of Concrete into the Canoe
Notes: Then the final layer of concrete was placed and the bulkheads were installed. Each of the bulk heads were three feet in length and a rod was used to ensure that the concrete was consolidate around the bulk heads as shown in Figure 37. Figure 38 demonstrates the placement of the second layer of concrete into the canoe (Colored White).

## Slide 33: Task 5: Final Canoe Construction Cont.
Figure 39: Installing Frame for Cure Chamber​
Figure 40: Installing Plastic Film over Frame of Cure Chamber
Figure 41: Image of Humidifying Efforts in Cure Chamber
Notes: Once the canoe had been constructed the team set up a curing chamber around the canoe made up of PVC pipe and plastic sheeting as seen in Figure 39 and 40. Four humidifiers were placed inside the chamber so that the concrete in the canoe had enough moisture to cure correctly. The humidifying efforts are shown in Figure 41.

## Slide 34: Task 5: Final Canoe Construction Cont.
Figure 42: 14-day Removal of Mold
Figure 43: Supporting The Canoe After Initial Removal of the Mold
Notes: Shown in Figures 42 and 43 is the canoe removed (mostly) from the canoe. The canoe was place back into the mold after release so that the inside of the canoe could be sanded with ease and provide support to the canoe.

## Slide 35: Task 6: Conference Deliverables
  A virtual conference was held
  Only the Technical Proposals were scored
  NAU Placed 9th out of 18 schools
Figure 44: Cover Page of Conference Report
Notes: Due to the world events the conference was changed from a full-fledged conference to a virtual conference. This means that only the reports were scored. Figure 44 illustrates the Cover page of the Conference Report Submitted. NAU placed 9th out of 18 schools.

## Slide 36
  Social Impacts:
Elementary School Field Trip
Networking with Suppliers
Economic Impacts:
Decreased Material Use = Lower Cost of Construction
Environmental Impacts:
Utilization of Recycled Material
Reusing Foam Pieces from Past Canoe Molds
Project Impacts
Notes: For the social impacts of this project, we were given the opportunity to teach an elementary class about our project. We answered questions and displayed actual samples of the mix for the canoe. This allowed us to show the importance of engineering to these children.
During the length of this project, we also got the chance to increase the supplier network that the team has at their disposal.
Economic Impacts for the project was the development of a shorter canoe, which in return needed less material for the project, which decreased the cost of the canoe.
For Environmental Impacts, the utilization of recycled material and reusing Foam Pieces from past canoes helped the canoe be more environmentally sustainable.

## Slide 37: Hours Per Task
Chart: 
| Mix Design | Hull Design | Structural Design | Construction | Concference Deliverables | Capstone Deliverables | Project Management
 | 234 | 52 | 134 | 293 | 170 | 80 | 87
Notes: The total hours to complete this project was 960 hours. This is less than predicted since some of the conference deliverables were not completed due to the conference being cancelled.

## Slide 38: References
[1] NCCC, Asce.org, 2019. [Online]. Available: https://www.asce.org/uploadedFiles/Conferences_and_Events/Event_Subpages/Content_Pieces/2020_nccc_request_for_proposals-rules.pdf. [Accessed: 26- Nov- 2019].

## Slide 39
Thank You!