## Slide 1: Metal 3D Printer Final Testing Results
Nathan Krikawa, Nolan Hann

## Slide 2: Project Description
Overview:
Commissioning of Concept Laser Mlab Cusing R metal 3D printer
Donated by Honeywell to NAU’s ME department for the IDEA Lab
Our Job:
Install and restore printer to proper functionality.
Evaluate printed specimen against machined counterparts
Print final part as part of assembly using topology optimization
Create instruction manual for training purposes in preparation for work orders and ME286L curriculum expansion
Figure 1: Concept Laser Mlab Cusing R
Figure 3: Redesigned aluminum gripper
Figure 2: Selective laser melting
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 3: Design Requirement Summary
# | Requirement | Units | Targets
ER1 | Materials Tested | Al, SS 316L, Ti, Bronze | One
ER2 | Final Print Material | Al, SS 316L, Ti, Bronze | SS 316L
ER3 | Final Print Volume | mm^3 | <90x90x80
ER4 | Power | V, A | 240V, 16A
ER5 | Inert Gas | N, Ar, bar, purity | 2 bar Ar purity >=2.5
ER6 | Young's Modulus Tested | GPa | 193
ER7 | Dog Bone Size | mm | 65
ER8 | Airtight Gas Supply | N/A | No audible leak
ER9 | Build Plate Alignment | N/A | Even material distribution
ER10 | Printed Part Tolerance | mm | ±0.2mm
# | Requirement | Description
CR1 | Ease of Use | Easily accessible to IDEA Lab managers, Instruction manual and supplementary instructions at hand
CR2 | Safety | Printer fully and properly installed, safety signs posted, PPE available, instruction manual at hand
CR3 | Time | Fully installed by the end of the spring 2025 semester
CR4 | Successful Installation | Printer fully operational, all technical issues addressed
CR5 | Tensile Test Results | All test specimen tested; all results analyzed
CR6 | Final Part and Assembly | Final part printed and assembled into greater assembly
CR7 | Instruction Manual | “First print” instruction manual complete with comprehensive steps and files attached
Engineering Requirements
Customer Requirements
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 4: Top Level Testing Summary
Experiment/Test | Relevant DRs | Testing Equipment Needed | Other Resources
EXP1 - Test Print | ER2 - Final Print Material (SS 316L) ER4 - Power ER5 - Inert Gas ER8 - Airtight Gas Supply ER9 - Build Plate Alignment ER10 - Printed Part Tolerance (±0.2mm) CR2 - Safety CR4 - Successful Installation CR6 - Final Part and Assembly CR3 - Time | Small tube Dial gauge indicator Shim Calipers | Rail system to slide dial gauge indicator along build module
EXP2 - Tensile Test | ER2 - Final Print Material (SS 316L) ER6 - Young's Modulus Tested ER7 - Dog Bone Size CR5 - Tensile Test Results CR3 - Time | Tensile test equipment Calipers | 
Test Summary Table
EXP1 – Test Print
Gas Leak Test
Build Module Trials
Shim Alignment
Test Print and Tolerance
EXP2 – Tensile Test
Tensile test machined specimen alongside printed specimen and compare
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 5: Detailed Testing Plans
EXP1 – Test Print
EXP1.1 – Gas Leak Test (50%)
Using 1” copper tube to detect audible leakage around gas tank, supply hose, and build chamber door.
EXP1.2 – Build Module Trials (100%)
Testing remaining 4 build modules for operation and alignment.
Figure 4: Door Seal Latch
Figure 5: Duct Taped Door Seal Latch
Figure 6: Build Modules
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 6: Detailed Testing Plans
EXP1 – Test Print
EXP1.3 – Shim Alignment (100%)
Leveling build plate using brass shims between build plate and build chamber
EXP1.4 – Test Print and Tolerance (20%)
Print complete part and test dimensions for tolerance ±0.2mm
Figures 8 & 9: 2nd Benchy Print
Figure 7: Test Shims
Figure 10: Level Build Plate
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 7: EXP1 Results
EXP1.1 – Gas Leak Test (50%)
All audible leakage fixed with duct tape, waiting on new build chamber door latch.
EXP1.2 – Build Module Trials (100%)
All modules tested, only one operable.
EXP1.3 – Shim Alignment (100%)
Build plate leveled, shimming process optimized.
Must be leveled between each print.
Field service required to fix build chamber z-axis elevator.
Part | Dimension | Expected (mm) | Actual (mm) | Difference (mm)
Overall | Width | 19.22 | 19.04 | 0.18
 | Length | 37.2 | 37.24 | -0.04
Roof | Length | 14.26 | 14.13 | 0.13
Cargo | Width | 7.44 | 7.27 | 0.17
EXP1.4 – Test Print and Tolerance (100%)
Benchy printed successfully, tolerance of ±0.2mm achieved.
Major dimensions compared to those from the Benchy website.
Model was scaled down to 62% for the print, and expected values are 62% of original model values.
Table 1: Benchy Tolerance test
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 8: Detailed Testing Plans
EXP2 – Tensile Test
EXP2 – Tensile Test (100%)
Tensile test specimen are placed in the device, then are slowly strained using increasing force until failure.
EXP2.1 (100%)
Machined specimens tested in room 101, tensile testing following E8/E8M and results graphed.
EXP2.2 (100%)
Printed specimen tested in room 100, similarly following E8/E8M and results graphed.
Figure 11: Testing Animation
Figure 12 and 13: Machined and Printed Specimen
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 9: EXP2 Results
Specimen Name | Max Engineering Stress [GPa] | Young's Modulus [GPa] | Yield Strength [MPa]
No Color Subtractive | 0.7642 | 96.9440 | 331.5659
Blue Subtractive | 0.8122 | 84.2820 | 412.3016
Jim Subtractive | 0.8970 | 82.5530 | 544.9523
No Color Additive | 0.8362 | 83.1530 | 504.0858
Blue Additive | 0.8779 | 82.0070 | 553.3102
Black Additive | 0.8623 | 83.5080 | 509.1423
Subtractive Avg. | 0.8245 | 87.9263 | 429.6066
Subtractive Range | 0.1329 | 14.3910 | 213.3864
Standard Deviation | 0.0673 | 7.8572 | 107.7406
Max | 0.8970 | 96.9440 | 544.9523
Additive Avg. | 0.8588 | 82.8893 | 522.1795
Additive Range | 0.0417 | 1.5010 | 49.2244
Standard Deviation | 0.0211 | 0.7845 | 27.0783
Max | 0.8779 | 83.5080 | 553.3102
Table 2: Tensile Test Results
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 10: EXP2 Results
Graph 1: Tensile Testing
Chart: Stress vs. Strain
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 11: EXP2 Results
Table 15: Offset Top and Bottom
Figure 14: Necking with Fracture
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 12: EXP2 Results
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 13: Printer Demo
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 14: Specification Sheets
Engineering Requirement | Target | Tolerance | Measured/Calculated Value | ER met? (Yes or No) | Client Acceptable (Yes or No)
Materials Tested | One | N/A | One | Y | Y
Final Print Material | SS 316L | N/A | SS 316L | Y | Y
Final Print Volume | <90x90x80 | No Tolerance | <90x90x80 | Y | Y
Power | 240V, 16A | >=240V | 240V, 16A | Y | Y
Inert Gas | 2 bar Ar purity >=2.5 | No Tolerance | 2 bar Ar purity >=2.5 | Y | Y
Young's Modulus Tested | 193 | N/A | Subtractive: 87.9263 Additive: 87.9263 | N | Y
Dog Bone Size | 65 | +-0.1mm | 65 |  | 
Airtight Gas Supply | No audible leak | No Tolerance | No audible leak | Y | TBD
Build Plate Alignment | Even material distribution | No Tolerance | Even material distribution | Y | TBD
Printed Part Tolerance | ±0.2mm | Same as Target |  | Y | Y
Customer Requirement | CR Met? (Yes or No) | Client Acceptable (Yes or No)
Ease of Use | Y | Y
Safety | Y | Y
Time | Y | TBD
Successful Installation | Y | TBD
Tensile Test Results | Y | Y
Final Part and Assembly | N | TBD
Instruction Manual | N | TBD
CR Summary Table
ER Summary Table
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 15: QFD
Notes: Overview:
Installing and Troubleshooting a M100LabR Concept Laser PBF Printer
Printing and evaluating parts and specimens (ie Stress-Strain, Thermal Management)
Creation of a user manual and short curriculum for ME286L
Included is the printer itself, powder mixer, powder trolley, and various powdered alloys for use with the printer
Location of set-up: CEIAS IDEA Lab, Room 116A

## Slide 16: Thank You!
Any Questions?